SPECIFICATION

## Comfort Zone™ Trouser

### A Top Brass® professional uniform

STYLE # & COLORS:

MALE			FEMALE

641MNV – LAPD navy	641FNV – LAPD navy

STYLE:  Uniform trouser, two quarter top pockets, two hip pockets, two cargo pockets, zipper fly front, seven beltloops, 2” elastic waistband with 4-bead silicone, crotch lining, French fly, triangular bartacks, set-in belt loops, expandable waistband at both side seams.

- FABRIC SUMMARY:

- Contents: 68% polyester

- 32% CoolMax®

- Construction:  Warp = 83, Filling = 61

Yarns:

Warp: 2-ply, 150 denier polyester

Filling A: 300 denier T400 elasterell-p (CoolMax), wrinkle resistant

Filling B: 2-ply 150denier polyester

Weave: 2x1 right hand twill

Weight:  11.66 ozs./linear yd. (60”)

7.0 ozs./sq. yd.

Stretch: 16% comfort stretch in the filling yarns

Dying: Vat dyed

Finish: Nano-dry™ technology provides comfort of cotton with strength          and performance of synthetics.  Features superior moisture management technology.

FABRIC DETAILS:

Test Name, Reference and KTEST #	Test Detail	Specification	Applicable to:

*	Colorfastness to Abrasion (Frosting)	1200 cycles	> 3.5	Spun Fabrics only

AATCC 119

A-01

*	Colorfastness to Crocking	Dry	> 4.0	All dark shades

AATCC 8	Wet	> 3.0	All dark shades

A-03

Optical Migration		No Discoloration	Frame applied Optical only

A-04			      Development Lots and Process Changes

*	Colorfastness to Light	20 hours	> 4.0	All lots

AATCC 16 - 1993 option A

A-05

*	Colorfastness to Perspiration - Acid	Shade Change	> 4.0	All lots

AATCC 15	Staining	> 3.0	Grade only Cotton and Polyester fibers

A-06

*	Colorfastness to Washing - IIA	Shade Change	> 4.0	All lots

AATCC 61 - 1993	Staining	> 3.0	Grade only Cotton and Polyester fibers

A-08

*	120oF Wash Shrinkage 	3 Wash/Dry cycles	< 3.0%	All lots

B-01	at 120oF	< 4.0%	Poly/wool, Poly/Rayon and Nylon

Test Name, Reference and KTEST #	Test Detail	Specification	Applicable to:

*	Press Shrinkage	15 sec. at 325oF	< 3.0%	All Lots

B-03

Appearance After Laundering	3 wash/dry cycles	> 3.5	Development Lots Only

C-01	at 120oF

Brush Pilling		> 3.0%	Spun Only

ASTM D3511

C-02

*	Pilling - Random Tumble	60 min.	None	Development Lots Only

ASTM D3512

C-03

*	Roughing and Pilling        original	15 min.	> 4.0	All lots

C-05                             	60 min.	> 3.0

3X at 120oF	15 min.	> 4.0

60 min.	> 3.0

*	Seam Slippage		> 20 lb.	Fabric weight < 3.0 oz./yd2

ASTM D434		> 30 lb.	Fabric weight > 3.0 oz./yd2

C-06

*	Stretch and Recovery	Stretch	Varies with Style

ASTM D 3107	Non-Lycra Recovery (30 min.)	< 5.0%	Non-Lycra Styles with Stretch > 20%

C-07	Lycra Recovery (60 min.)	< 4.0%	Lycra Styles

*	Tensile Strength		> 30 lb.	Fabric weight < 3.0 oz./yd2

ASTM D 5034		> 50 lb.	Fabric weight > 3.0 oz./yd2

C-09

Texture Distortion	4 lb. load	< 0.10 in.	Menswear

ASTM D1336	2 lb. load	< 0.15 in.	Womenswear

C-10

*	Elmendorf Tear 		> 1000g	Fabric weight < 3.0 oz./yd2

ASTM D1424		> 1500g	Fabric weight > 3.0 oz./yd2

C-04

Flammability - 16 CFR 1610		Class 1	Hand Standards

F-1

Mark Off	Varies by Style	Pass

* Tests that are required when applicable on Color Standard lots.

POCKETS: There shall be two (2) front quarter top styled pockets.  The swing type pocket bag shall be 7 ½” deep.  The pocket shall angle forward 1 ½ to 1 ¾” at the top.  The pocket facing attached to the side seam shall be 2 ¾” wide at the top.

There shall be two (2) rear hip pockets.  The left shall have a button and tab closure.  They shall be 5 ¼” wide.  The left pocket shall have a button and hole closure.  This shall be a Reece, double-welted style pocket.  The pocket bag shall be 6” deep.  These welts shall be topstitched top and bottom.

There shall be a cargo pocket with flap on each leg, beginning 1-3/4” below the bottom of the quarter top pocket. The pocket shall measure 7 ½” wide and 9” high from the bottom of the pocket to the top of the flap.  There shall be a center pleat 1-1/2” wide.  The pointed style flap shall measure 7-1/2” wide, 2-1/2” at the sides and 3-1/2” at the center point.  The sides of the flap secured by hidden Velcro.

There shall be a hidden #3 nylon coil zipper behind the pocket flap for entry into a separate pocket behind the main cargo pocket.  There shall be a second hidden #3 nylon coil zipper along the front vertical edge of the pocket.  This zipper shall enter the same pocket area as that of the top zipper behind the pocket flap.

POCKETING:  Shall be 50% polyester, 50% cotton, 260-weight drill and shall withstand all pilling for a minimum of 30 wash cycles.  Color shall be black.

WAISTBAND:  The outside shell waistband shall be 2” wide. There shall be a canvas backing to the waistband to give it body & support.  The inside waistband curtain shall be made of 2 ½” wide elastic, grey in color with a 4 bead royal blue silicone.  This silicone shall help prevent the shirttails from easily sliding out of the waistband.  The elastic shall extend from the left front, around the back to the right front.  This is to be no break at the back center seam.   The elastic curtain shall have a stretch binding along the entire top edge.

The elastic shall be sewn to the outside waistband except for approximately 3” at each quarter top pocket to facilitate the extension (stretch) of the waistband.  The front left and right waistbands shall taper immediately after the quarter top pocket opening and insert into a tunnel opening at each side seam into the rear waistband, approximately 2 ½” in length.  It will then be attached to 1” wide elastic webbing.  This webbing shall be approximately 2” in length and be sewn to the waistband underneath the side seam belt loop.  The front waistbands will expand into and out of these tunnels a minimum of 2” on each side.

BELTLOOPS:  There shall be an average of seven (7) belt loops (except the smallest sizes will have 5 and the largest 9 ea.).  These shall be of shell material and interlined.  They shall be set into the top and bottom of the waistband seam.  They shall be ¾” wide and 2” long.

FRENCH FLY: There shall be a French fly, made of shell material.

CROTCH LINING: There shall be 2/4 front crotch lining, made of pocketing material.  These shall have folded edges, and made of double ply material.

ZIPPER: Shall be brass and of good commercial quality.  Shall withstand all laundering and pressing for the life of the garment.  Shall be self-locking style.

INSEAM:  Shall be proportionally graded to average 37” open bottom.

SEAMS:  Both the inseam and outseam shall be serged and pressed open.

BARTACKS: There shall be straight bartacks at the top and bottom of the quarter top pockets, the base of the fly and one bartack securing the inside of the right fly to the left fly about 1” above the bottom of the zipper. There shall be triangular bartacks at the ends of the hip pockets.

THREAD:  All thread shall be color fast, polyester core, two-ply.  This shall identically match the fabric color.

FINISHING:  This garment shall be finished in a first class workmanlike manner with all loose threads removed.  The omission or apparent omission of any wording or specifications shall mean that only the highest quality industry standards shall be used on all fabric and component parts including labor.  Where there may be a discrepancy between the standard sample and the written specification, the detail of the standard sample shall prevail.

LABELS:  All labels will be permanent to withstand repeated cleanings for the life of the garment.  The following labels shall be applied:

MAIN LABEL:  This shall identify the manufacturer either by name & location, registered trademark or WPL or RN number as required by the Federal Trade Commission.

CONTENTS/CARE/SIZE LABEL:  There shall be an additional label clearly showing the fabric contents, laundering instructions and garment size.

SIZES:

Male:	28-38 (all sizes)

40-54 (even sizes)

Above 54 as needed

Female: 4-28